## Slide 1: KSCT Fall Meeting
Sep 9th 2021
Theoretical Separation Feasibility of Zeolites for Gas Sweetening Process
Seongbin Ga
Pusan National University

## Slide 2: How Adsorption Processes Work
Pressure (bar)
Uptake (mol/kg)
Adsorption phenomena on adsorbent surface
Adsorbent particles
Adsorption at condition 1:
Desorption at condition 2:
High pressure (), Low temperature ()
Low pressure (), High temperature ()
Pressures swing adsorption (PSA) process
Temperature swing adsorption (TSA) process
Compressed feed
Raffinate product
Low pressure exhausting
Increased pressure
Decrease pressure
Adsorption isotherm curve (key data)

## Slide 3: Cyclic Operation of Adsorption Process
Pressure (bar)
Uptake (mol/kg)
Adsorption isotherm curve (key data)

## Slide 4: Cyclic Operation of Adsorption Process
time (sec)
Cycle configuration
Step 1:
adsorption
Step 2:
pressure equalization (P↓)
Step 3:
blowdown
Step 4:
evacuation
Step 5:
pressure equalization (P↑)
Step 6:
re-pressurization
Simulation results
e.g. CO2/N2 separation (gas phase concentration)
Efficiency (CO2 ton/ GJ)
CO2 purity (mol/mol)
Process-level performance

## Slide 5: Problem 1: CPU time
Suppose we have many adsorbents to evaluate.
For each adsorbent, we need
1) Dynamic simulations (min-level)
Ref) Saberimoghaddam, & Khebri, J. Chemometrics, 2016
Mass, momentum, and energy balance equations
Cyclic steady state (CSS) conditions
2) Cyclic steady state search (hr-level)
3) Design & operation optimization (day-level)
Operation optimization example
Adsorbent 1  optimal operation set 1
Adsorbent 2  optimal operation set 2
uptake
0
…
…
CSS swing

## Slide 6: Problem 2: Limited information
For the dynamic simulation for the PSA process, a variety of adsorbent properties are essential:
Activated carbon
Zeolite
MOF
Various materials
etc.
…
Adsorption isotherm data, heat of adsorption, mass/heat transfer coefficients, heat capacity, density ….
Adsorption isotherm data
Most of them are rarely available,
especially when they are:
newly discovered or
newly developed or
newly synthesized
Molecular simulations
Synthesis of adsorbents
Ref) Lee, Kim, and Ahn, KJChE, 2013
Pressure (bar)
Uptake (mol/kg)
Uptake (mol/kg)
Pressure (bar)
…
Adsorption isotherm curves = The first property they can obtain.

## Slide 7: Idea: Ideal PSA Process
Inspired by McCabe Thiele method or Fenske equation
[Shortcut method: ideal PSA process]
For distillation column
Equilibrium info.
Feed conditions
Target purity
Required process (operation or design)
For pressure swing adsorption (PSA) column
Isotherm info. (Usually measured first)
Feed conditions
Target purity
Required process (operation or design)
?
(Available for material developers)

## Slide 8: Idea: Ideal PSA Process
[Shortcut method: ideal PSA process]
For pressure swing adsorption (PSA) column
Isotherm info. (Usually measured first)
Feed conditions
Target purity
Required process (operation or design)
?
(Available for material developers)
Derivation of the method (formula) starts from a set of assumptions (idealization):
Two gas components
No dispersion: clear saturated region boundary
Two periods: saturation & desaturation
Full capacity of the adsorbents
Always in solid/gas equilibrium
No effect of void volume
mol. frac.
Axial (m)
Unsaturated region
Saturated region
Saturation period
Desaturation period
20/32

## Slide 9: Formula: Ideal PSA Process
Asymptotically approach
[Converges to a certain value]
(Purity)—(operating pressure) graph
Upper limit of purity (purity cannot exceed this)
Advantages of them:
Reflective of the application to the PSA process
Easy to use and requiring only isotherm parameters
Small computational cost (compared to PSA simulation time: ~2000 sec with successive substitution )
S. Ga et al., Comput. Chem. Eng., 2017
Efficiency
Purity
New shortcut evaluation method
Proposed in

## Slide 10: Multi-component Case: CH4/H2S/CO2
Natural gas sweetening process (feed gas contains CH4/H2S/CO2):
Different adsorbents can be classified into three cases.
Feed gas ()
CH4
CO2
H2S
Natural gas production ()
Adsorbent A
Feed gas ()
comes first
Adsorbent B (H2S leading case)
Feed gas ()
comes first
Adsorbent C (CO2 leading case)
(CH4 leading case)
Desirable cases

## Slide 11: Expansion Set of The Ideal PSA Method
Unsaturated
Saturated
Feed
Leading component concept
During the adsorption step, the saturated region is propagated by the feed gas.
The rate of saturation differs for each gas component.
From the ideal PSA concept, we can calculate the rate of saturation as:
Rate of the saturation for component ()
[Definition]
From the mass balance,
[Length of saturation region]
Therefore,
[Ratio of the rate] = [Ratio of length]

## Slide 12: Application to Zeolite Database
International Zeolite Association (IZA) database
            Database providing structural information of over 300 zeolites
            Data in the crystallographic information framework (*.cif) file
            Online available database
Ideal PSA simulation Results: Classifying zeolites of IZA database
(1) CH4 leading case (8 zeolites)
(3) CO2 leading case (83 zeolites)
(2) H2S leading case (255 zeolites)

## Slide 13: Visualization for Classification
CH4
CO2
H2S
Rs1 =
Rs2 =
CH4
H2S
CO2
CH4
Saturation region ratio
> 1
> 1
Feasible candidates
Different Saturation regions
- Graph
AEI-0
APC-1
CDO-1
JBW-0
MON-0
RRO-0
VSV-0
WEI-0

## Slide 14: Conclusion
mol. frac.
Axial (m)
Unsaturated region
Saturated region
Saturation period
Desaturation period
Based on an ideal PSA process, shortcut evaluation method has been developed.
The ideal PSA shortcut method is extended to the multi component gas separation system.
Using IZA database, the separation feasibility was tested for 346 zeolites, and 8 zeolites were found to be feasible.

## Slide 15
Seongbin Ga School of Chemical Engineering Pusan National University (PNU) Republic of Korea
Email: sga00@pusan.ac.kr

## Slide 16: Validation: Ideal PSA Process
In
S. Ga et al., Comput. Chem. Eng., 2017
I theoretically derived the method, and roughly validated by comparing with the rigorous (dynamic) simulations.
PSA dynamic simulation (non-ideal) | Selectivity
0.1992 | 100~300
0.2601 | 20~26
0.333 | 7~25
>
>
>
>
>
>
>
cf) Working capacity (1~15bar)
A: 2.2mol/kg
B: 0.95mol/kg
C: 8.1mol/kg
Comparison of the sorbents (if target purity = 0.5)
Cu-BTC
BPL (AC)
Zeolite 13X

## Slide 17: Validation: Ideal PSA Process
Realff group in Georgia Tech has validated with many adsorbents.
You, Sen et al., Applied Nano Mat. 2020
Shortcut method: ideal PSA process
Rigorous simulations: dynamic model

## Slide 18
Application of the Method

## Slide 19: Application 1: CO2 Capture
Use of molecular simulation (Co-work with Jihan Kim’s group in KAIST)
…
Y. Chung, et al., Science Advances, 2016
Sorbent structure information
CoRE MOF Database: Web available library of MOF structures
Property parameters
isotherm parameter library database
Shortcut evaluation method
Ranking of the adsorbents for given…
Isotherm information
Feed conditions
Target purity

## Slide 20: Application 1: CO2 Capture
In a idealized pressure swing adsorption (PSA) process for CO2
Thousands of candidates: - CoRE MOF (about MOFs) - IZA (about zeolites)
Operating conditions:
- -
-
Feed conditions:
Product out
Packed sorbents
-
- -
Feed in
Parameter library from molecular simulations
Graphical user interface (GUI) for sorbent evaluation

## Slide 21: Application 1: CO2 Capture
Input GUI for sorbent ranking
Example ranking result
Ranking of adsorbents with quantified performance: efficiency (CO2 ton/ GJ)
Candidates that cannot achieve the target purity and their upper bound list ()
Graphical user interface (GUI) for sorbent evaluation

## Slide 22: Application 1: CO2 Capture
Graphical user interface (GUI) for sorbent evaluation
Available in File Exchange webpage (MathWorks):
https://kr.mathworks.com/matlabcentral/fileexchange/71661-general-adsorbent-library-and-evaluation-gale
S. Ga et al., Comput. Chem. Eng., 2020
Proposed in

## Slide 23: Application 2: MOFs for Ethane/ethylene Separation
Molecular simulations of 6,830 metal organic frameworks (MOFs) from CoRE MOF database
Kang et al., Adv. Sci., 2021
Reported in
Dr. Yongchul Chung
Dr. Seongbin Ga
Dr. Chang Seop Hong
Shortcut method for VSA process
Ethane/ethylene Isotherms
Best MOFs
Synthesize of top 3 MOFs, measurement, and durability test
Compare with recently reported MOFs
Durable MOFs measured data

## Slide 24: Application 3: MOFs for SF6/N2 Separation
Cha et al., Chem. Eng. J., 2021
Reported in
[Use of CoRE MOF database again for SF6/N2 separation]
Based on the molecular simulation results (isotherm curves of 2,890 MOFs),
we found any of MOFs cannot achieve 90% SF6 with a PSA process.
Product SF6 purity for different adsorbents
Then, we need to use cascade PSA with two trains:

## Slide 25: Summary
Shortcut evaluation method
Applications of the shortcut evaluation method
Shortcut evaluation method has been suggested by assuming an ideal PSA process.
The method provides quick evaluation with limited information.
CO2 mol. frac.
Axial (m)
Unsaturated region
Saturated region
Saturation period
Desaturation period
Adsorbents for CO2 capture can be evaluated, which is also available in a GUI form.
MOF screening work found Ni(IN)2 for C2 separation, whose durability and separation performance have been tested.
Through the shortcut method, we found SF6 separation requires cascade PSA process with at least two PSA trains.

## Slide 26: Table of Contents
1. Shortcut Adsorbent Evaluation Method
1. How adsorption processes work
2. Problems of the existing methods
3. Breakthrough: shortcut method (ideal PSA process)
4. Validation of the process
2. Applications to Different Areas
1. For CO2 capture and graphical user interface (GUI)
2. Ethane/ethylene (C2) separation
3. SF6 capture